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Training Requirements/Standards: CSCS Card

	Task, Process or Activity to be undertaken:

	
Justification: 

Damage left by historic scaffolding ties. 


	Sequence and method of Work:

	
Scaffold Fixing Repair

Historic - Steel Socket 

· Carefully drill around the scaffold fixing using a small diamond core bit slightly bigger than the scaffold fixing.

· Using a mallet and chisel shock the fixing causing the core to snap and remove the fixing from the brick or stone unit. 

· Use a hoover to suck out as much of the dust and debris as possible before using an air pump to blow out the last remaining amounts.

· Well wet the hole with clean water and apply a lime based restoration mortar which is to be a mixture of washed sand, silver sand and NHL3.5 lime including a colour tone as required. The mortar is to be tamped in place, left proud and allowed to cure slightly. 

· Prior to a full cure the mortar is to be dressed back using brushes and sponges back to the face of the brick/stone and left with a finish to match the surrounding masonry. 

· Once final cure has occurred then any remaining construction dust or run down is to be cleaned off from the surface of the stone block and left ready for handover / inspection.

· Due to the small sizes of the holes and the level of finish that we can achieve using a stone restoration repair we feel this is the best approach to make good the scaffold fixing holes rather than replacing full brick or using stone plugs/indents. 

Nylon Socket

Nylon insert with fully retrievable steel tie. 
 
· Drill a 14mm hole, with a 12mm tie, that will require matching to existing upon striking the scaffolding.
· Method of repair to be equivalent to historic steel socket. 



	Programme Time and Duration:

	
Anticipated that the works will be agreed with Stone Central & Seddon Construction to align with the building programme.

	Supervisory Arrangements including Deputy:

	
The Stone Central (NW) Ltd foreman is to continually monitor the work area to ensure there are no new hazards. The Stone Central (NW) Ltd foreman is to complete their Site diary on a daily basis and ensure the Site Attendance records are kept up to date.  
Training Requirements/Standards: SSSTS


	Monitoring Arrangements:

	
Quality monitoring to be conducted by Stone Central throughout the procedure.


	Plant and Equipment:

	
Mallet, Chisels, 5-inch grinder, drill, small breaker, leads, hoover.



	Lifting / Handling:

	
[image: ]Movement of bags of debris. 





	Health Hazards / Controls / CoSHH :

	
CoSHH – N/A

Written risk assessments for associated tasks are enclosed. Working on a tube and fitting scaffold, abrasive wheels, use of power tools, use of hand tools, working on a scaffold, working in close proximity to rats.


	PPE Requirements:

	
[image: ]

	Access / Egress & Workplace:

	
Our workers and the equipment they are to use will gain access to the work area via the main site entrance located on High Street and then the access routes to the main external scaffold via the designated pedestrian walkways within the confines of the site.



	Specific Control Measures:

	
Operatives to have CSCS cards and supervisor to have SMSTS. 
All operatives to wear full PPE – hard hat, high vis vest, steel toe capped boots and gloves. If asked to cease works, make sure the work area is safe and then do so before contacting a supervisor. No eating permitted on site apart from within the welfare area. Sign in and out each time when entering or leaving site using the biometric system. Scaffold to be certified for use and deemed safe for conducting work by the Site Agent. The listed status of the building is to be explained to any operative from Stone Central starting work on the project so that they follow standard guidelines when working on such a project. Goggles, ear defenders and dust mask to be used when conducting the cutting works along with use of a hoover.


	First Aid:

	
All Stone Central (NW) Ltd injuries must be reported to the foreman who will then inform the Principal Contractor without delay.




2 of 4

image1.png




image2.png
B OMO®EOE




image3.png




