Midland Hotel

Terracotta Repairs To Mount Street Entrance

- Identify water and power supplies as near as possible to our work area.

- Ensure that all drains are suitably protected to prevent any blockage.

- Identify areas of masonry/fiberglass to be cut back and restored.

- Carefully remove any redundant fixings using hand pliers and drills.

- A sample area to be prepared prior to undertaking the works for approval by the

- architect.

- Carefully using feint cutter, make an insertion along the fiberglass restoration to allow the insertion of chisel

- Using Masons hand tools cut back the defective fiberglass repair ready to receive repair.

- Where necessary wet masonry to ensure a good bond for the repair mortar.

- Apply build-up of mono-light flexible repair mortar to the masonry to get the shape and mould of the existing terracotta. Profile

- Any Deep pockets to be built up with armature

- Introduce false jointing to replicate existing (this can then be pointed up in the approved pointing mix in a later date)

- Thoroughly brush down the exposed areas to remove loose dust and wash down area to remove all particles.

- Apply degreasing agent prior to finishing coast

- Once clean, apply sealant to achieve a glossy finish. This may have to be repeated multiple times to acquire the right finish

- Sand down to a smooth finish for any high spots or runs on the sealant ready for colour application

- Apply colour application with airbrush feathering in to match surrounding terracotta, this step will be repeated until desired finish is achieved.

- Final glass coat to be applied for finish then cured with heat gun to a baked finish

- Upon completion of repairs, all original joints if effected within the area of restoration to be cut out to the full depth of repair and point with approved mortar mix.

- On completion of restoration works, strip all protection and debris and remove from site.