Midland Hotel

 Terracotta Repairs To Mount Street Entrance



1. Identify water and power supplies as near as possible to our work area.

2. Ensure that all drains are suitably protected to prevent any blockage.

3. Identify areas of masonry/fiberglass to be cut back and restored.

4. Carefully remove any redundant fixings using hand pliers and drills.

5. A sample area to be prepared prior to undertaking the works for approval by the 
6. architect.

7. Carefully using feint cutter, make an insertion along the fiberglass restoration to allow the insertion of chisel

8. Using Masons hand tools cut back the defective fiberglass repair ready to receive repair.

9. Where necessary wet masonry to ensure a good bond for the repair mortar.

10. Apply build-up of mono-light flexible repair mortar to the masonry to get the shape and mould of the existing terracotta. Profile

11. Any Deep pockets to be built up with armature

12. Introduce false jointing to replicate existing (this can then be pointed up in the approved pointing mix in a later date)

13. Thoroughly brush down the exposed areas to remove loose dust and wash down area to remove all particles. 

14. Apply degreasing agent prior to finishing coast

15. Once clean, apply sealant to achieve a glossy finish. This may have to be repeated multiple times to acquire the right finish 

16. Sand down to a smooth finish for any high spots or runs on the sealant ready for colour application

17. Apply colour application with airbrush feathering in to match surrounding terracotta, this step will be repeated until desired finish is achieved.

18. Final glass coat to be applied for finish then cured with heat gun to a baked finish

19. Upon completion of repairs, all original joints if effected within the area of restoration to be cut out to the full depth of repair and point with approved mortar mix.
20. On completion of restoration works, strip all protection and debris and remove from site.




