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	Applications
	Structure and Operation

	For purification of supply air, exhaust air and circulating air streams from harmful gases, steams and bad smells in:
· Canteen kitchens, museums, waste recycling centres
· Hospitals, laboratories, computer areas
· 	Chemical industry, paintshops, airports, petrol stations, parking garages
	· Solid carbon
· Strong robust galvanized frame
· 	Humidity resistant up to 70% r. h.
· 	Temperature resistant up to max. 40°C



	Versions
	Contact time (Dwell Time)

	· V-Formation
· Standard Duty
· Heavy Duty
· Removes hydrogen sulphide, ammonia, DMS etc.
	· 0.1 Second – 0.4 Second
· Please ask for recommendations on dwell time




	Tri-carb Safe Fit
	24x8x24
	Tri-carb Safe Fit
	3 x 24x8x24

	Dimensions
	595x198x595
	Dimensions
	595x595x595

	Gross Weight
	22.00KG
	Gross Weight
	66.00Kg

	Carbon Weight
	17.00KG
	Carbon Weight
	51KG

	Rated Velocity
	1266 M3/h
	Rated Velocity
	3800 M3/h

	Pressure Drop SD
	185Pa
	Pressure Drop SD
	185Pa




Tri-Carb Dimensions
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	TSF180912
	2
	18x18x12
	451x220x295
	6.5
	9.85
	473

	TSF240612
	2
	24x12x12
	595x146x295
	6.5
	8.80
	469

	TSF240812
	3
	24x24x12
	595x198x295
	8.68
	11.00
	625

	TSF180918
	2
	18x18x18
	451x220x451
	10.08
	13.85
	725

	TSF240618
	2
	24x12x18
	595x146x451
	9.98
	13.22
	719

	TSF240818
	3
	24x24x18
	595x198x451
	13.31
	16.55
	958

	TSF180924
	2
	18x18x24
	451x220x595
	13.31
	16.55
	958

	TSF240624
	2
	24x12x24
	595x146x595
	13.18
	16.68
	950

	TSF240824
	3
	24x24x24
	595x198x595
	17.58
	22.00
	1266



The above capacities are based on a 0.1 second dwell time. Please refer to the table below for the recommended minimum dwell times required for different applications and scale up accordingly. It should be noted that filtration performance will be improved by increasing the dwell times applied. The appropriate suffix should be added to the part number to specify the required grade e.g.
TRI240824CU50

	

	

	

	


	General Cooking
	0.1 – 0.2
	COL-A50
	OLA-50

	Spicy – Indian
	0.2 – 0.4
	COL-A50
	OLA-50

	Reduction of Kerosene
	0.1 – 0.2
	COL-A50
	OLA-50

	Reduction of Ozone
	0.1 – 0.2
	COC-A50
	OCA-50

	Diesel Fumes
	0.2
	SORB17
	SORB17

	Museum
	0.2
	Museum Grade
	CU-50

	Mortuary
	0.4
	Mortuary Grade
	FORM

	Ammonia
	0.3
	Ammonia Grade
	AMM



Other Applications
We can formulate gas phase filters for most applications, simply contact us with your enquiry. 
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