Condition 7:
(Specification of Mortar): 
NHL2 Lime mortar to stonework NHL3.5 Lime mortar to brickwork Mortar Specification: 3 parts local washed sand 1 part NHL 3.5 or 5 90ml black dye supplied from Womersley’s For the purpose of the sample the following measures were used: Sand – 1450ml Lime – 450ml Black Dye - 90ml 
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