Further to the submittal of the lead sample and joint welding please see below a working methodology for the leadwork weld repairs to the lead gutters.
 
Asses lead gutters for any cracks / defects.
Once we have found any areas where Cracks/ defects are present we will carefully remove the roof tiles surrounding the area of damaged lead and set them aside to be reinstated after the repair has been completed, In areas where coping stones are present we will again carefully remove and set aside to be reinstated after the repair has been completed,
All efforts will be made to protect the fabric of the building,
Once found clean a 100mm area around the defect using a shave hook scrapping back     the old lead to expose a new clean surface ready to weld a new patch of lead over the defect. 
To carry out this work there will be 2 operatives present, 1 to carry out the works and the other on fire watch whilst the works are in progress. 
A hot works permit will be required at the start of each working day and is to be signed off at the end of each day. 
Hot works must be completed 2hrs prior to operatives leaving site.
2no Fire extinguisher & a fire blanket will always be present.    
